| BRICK – PANELS JOINT ALIGNMENT SYSTEM |  |  |
| --- | --- | --- |

| NEOPOR -EPS- RIGID FOAM PANELS WHITE High Performance Insulation for our Brick-Tiles Characteristics data Joint alignment system EPS - Rigid Foam WLS035 (white) |  |  |  |  |  |  |  | Stand 04.2011 Date: 30. 04.2011 |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Neopor (EPS)-rigid foam | CFC-and HCFC-free, guaranteed quality |  |  |  |  |  |  |  |  |  |  |  |
| Properties: | Non-glowing, non-melting, and is not dropping off whilst burning, Biological harmless, non-rotting, recyclable, mould and mildew-resistant. |  |  |  |  |  |  |  |  |  |  |  |
| Apparent density | >25 kg/m² in accordance with DIN EN 1602 |  |  |  |  |  |  |  |  |  |  |  |
| Compressive strength at 10% compression | >100 kPa in accordance with DIN EN 826 |  |  |  |  |  |  |  |  |  |  |  |
| Rated value of thermal conductivity | λ 0,035 W/(m-K) in accordance with DIN EN 4108-4 |  |  |  |  |  |  |  |  |  |  |  |
| Application type | WAB in accordance with DIN EN 4108-10 |  |  |  |  |  |  |  |  |  |  |  |
| Construction material class With brick tiles | B1 in accordance with DIN EN 4102 System can be used up to 22 meter Other high on request |  |  |  |  |  |  |  |  |  |  |  |
| Temperature resistance | -30˚C to +110˚C -22˚F to +230˚F |  |  |  |  |  |  |  |  |  |  |  |
| Coating | no |  |  |  |  |  |  |  |  |  |  |  |
| Edge finishing | Head site stepped, sides with tongue and groove from thickness 30 mm |  |  |  |  |  |  |  |  |  |  |  |
| Dimension/Format | RF/WDF-123.5x54.5 cm NF-123.0x58.0cm DF-123.0x56.5 cm |  |  |  |  |  |  |  |  |  |  |  |
| Thickness rigid PUR in mm U-value (W/m²-K) R-value (m²-K/W) | 25 1,40 0,71 | 30 1,17 0,85 | 40 0,87 1,14 | 60 0,58 1,71 | 80 0,43 2.28 | 100 0,35 2.85 |  | 120 0,29 3,42 | 140 0,25 4,00 | 160 0,21 4,57 | 180 0,19 5,14 | 200 0,17 5,71 |
| Brick –tile type/dim. In mm | NF240x71x14/17, WDF 210/215x65x14/21, RF 240x65x14/17 DF240x52x14/17, other format /thickness on request |  |  |  |  |  |  |  |  |  |  |  |
| Brick –tile colours | See website www.brick-panels.co.uk |  |  |  |  |  |  |  |  |  |  |  |
| Admission | Isoklinker Z-33.46-936 Other technical details on request. Deutsches Institute fur Bautechnik. Berlin |  |  |  |  |  |  |  |  |  |  |  |
| Fourways ML 42 Valentines Road Ilford, ESSEX London IG1 4SA; Tel./fax: +44(0)20822271036 +44(0)7712284159 +44(0)7545966558 e.mail: info@brick-panels.co.uk www.brick-panels.co.uk. |

The above information is based on current knowledge and experience. No binding assurance in respect of certain  properties or suitability for certain applications must be read into our information. Patent rights and other proprietary rights must be observed if necessary.

Please note: As part of our continuing product development and improvement policy, we reserve the right to change product specifications without prior notice. Product colour may vary on screen so please visit the contact us page to order a copy of our product guide for more accurate colour specifications.

26.03.2013